## Slide 1
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · TECHNICAL TEXTILES KEYNOTE
Weaving Aramid Fibres
Engineering the limits of high-performance protective fabrics
PRESENTED BY
Ritesh · Ratanmoti Advance Textile
BHARAT TEX 2026 · ARAMID WEAVING
01 / 08

## Slide 2
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
02 / 08
THE PROBLEM SPACE · 01
If your product depends on aramid, the quality of its weaving is the quality of your product.
PARA-ARAMID
Strength & stopping power
Very high strength and stiffness — the fibre behind bullet-proof vests and armour.
META-ARAMID
Heat & flame resistance
Stays intact in fire and extreme heat — the fibre behind firefighter suits.
Ballistic armour
Firefighter kit
Aerospace
Filtration
Cut-resist gloves
High-strength ropes

## Slide 3
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
03 / 08
THE PROBLEM SPACE · 02
The loom must adapt to the yarn — not the other way round. Most suppliers never make that shift. We did.
Why Aramid Is So Hard to Weave
THE FIBRE…
…FIGHTS THE LOOM
Barely stretches (2–4%)
›
One small tension spike and the yarn snaps
Very stiff
›
Fights bending around every part of the loom
Slippery, high-friction surface
›
Rubs hard on metal and frays easily
Chemically inert
›
Ordinary sizing won't stick — it needs special coating
Brittle at sharp angles
›
Snaps where a normal yarn would simply bend

## Slide 4
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
04 / 08
THE PROBLEM SPACE · 03
Almost No Stretch — That Is the Whole Problem
Ordinary yarns (gold) stretch & forgive · High-performance fibres (teal) have no give
Wool
33%
Polyester
20%
Cotton
8%
Glass fibre
4.5%
UHMWPE
3.5%
Aramid
3.0%
Carbon fibre
1.6%
Ordinary yarn stretches and forgives. High-performance fibre does not — so there is no margin for error on the loom.

## Slide 5
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
05 / 08
THE PROBLEM SPACE · 04
Damage done on the loom is invisible there — it shows up later as your failure in the field.
Every contact point is a wear point.
HOW THE DAMAGE ADDS UP
Smooth yarn → tiny rubs → filaments split → surface frays. Tiny rubs pile up until the yarn loses its strength.
Stiff yarn fights every up-and-down of the loom — worst of all in dense, life-saving fabrics.

## Slide 6
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
06 / 08
WHY IT MATTERS
Three Real Failures — and the Defects Behind Them
Body armour that let a bullet through
A vest rated to stop the round simply didn't.
THE CATCH · The weave looked perfect — the fibre had quietly lost a third of its strength.
A fire coat that looked fine
Retired gear had lost most of its protective strength.
THE CATCH · You can't see the damage — so gear is retired by age, not by looks.
One broken thread in a parachute
A single fault can start a tear across the whole canopy.
THE CATCH · That is why the safety standard counts every defect.
IS 4726 · DEFECT ATLAS
24 graded weave defects
Broken ends & picks · floats · slubs · snarls · abrasion · holes · smashes · weak places · pin-holes · biased & bowed filling · selvedge faults · width — each graded Major or Minor. In the live deck these rotate automatically beside the case studies.

## Slide 7
RATANMOTI
ADVANCE TEXTILE
BHARAT TEX 2026 · ARAMID WEAVING
07 / 08
THE RATANMOTI ANSWER
We Know How to Weave These Fibres
WE HOLD THE YARN IN ITS SAFE WINDOW
SAFE WINDOW
Tension is held exactly in the safe zone — too low and the yarn goes slack, too high and it snaps. We keep it just right, automatically.
JUST RIGHT → clean weave, full strength retained
We don't force the fibre to fit the loom.
We build the loom around the fibre.
PROVEN ACROSS EVERY HIGH-PERFORMANCE FIBRE
Para-aramid
Meta-aramid
Carbon
Glass
UHMWPE
Tension, climate and machine health under closed-loop control — on every metre we weave.

## Slide 8
RATANMOTI
ADVANCE TEXTILE
Thank You
Questions & discussion
Ritesh · Ratanmoti Advance Textile · Bharat Tex 2026